Welding, Bonding, and the Design of Permanent Joints

Shigley Chapter 9

Outline

# Chapter 9:

### I. Rivets

- General

  - Efficiency  -- high (Compare w/ bolted joint) see diagram in class

  - Cost – Less than bolts and can be used with high speed riveting machines

B) Pretension

- Red hot when installed – old type structural rivets

- Installation mechanism mushrooms and cinches connections

C) Disadvantage – destructive disassembly (for permanent joints)

D) Types

- Tubular – Examples in class

- Blind – Examples in class

### II. Welding

- General – Metallurgy

- Welding potentially heat treats the base metal

- This process generally changes the metallurgical structure

- Can have a heat affected zone in the base metal outside of the welded region

- The head affected zone can have a significantly altered strength

- Steels that don’t heat treat are excellent candidates for welding example: carbon steels with < 0.3% carbon

- Weldable Materials – (OH in class)

- Low Carbon Steels – excellent candidates

- Alloy Steels – weldable but may require preheat/post heat

- Aluminum, etc.

- Welding Symbols – see pages 458-460

- Welding Geometry

- Butt weld  -- Examples in class

- Fillet weld – Examples in class

- Stress Analysis  -- general

- Always follow codes that pertain to the application

- Simple conservative model for fillet weld stress

  - Based on the shear stress at the minimum throat area

  - Equation for shear stress:

where At  is the minimum throat area = 0.707 hl

and h is the weld leg height and l is the length of the weld

use for tensile or shear applications

Example problems – in class

    - Torsion induced stresses --- see pages 464 – 468

    - Bending induced stresses --- see pages 469– 471

  - AWS and AISC code strength values and fatigue factors pages 472-473.

  - Some examples problems of static loaded weldments using tables 9.3 - 9.6.

- Resistance weld (spot welding, seam welding) p. 480

### III. Other Joining Methods

- Brazing and Soldering

- Surface preparation is important

- Include mechanical engagement if possible

- Temperature limit

- Adhesives

- Surface preparation is critical

- Include mechanical engagement if possible

- Enhance surface contact area * (see fig. 9-28)

- Good design practices for adhesive bonding (see fig. 9-32)

- Good design requires that adhesive joints be constructed that the adhesive carries load in shear rather than in tension across the bond surface.

- Temperature limit

* “personal experience story”